| Coating |  |  |  |  |  | Workpiece Material |  |  |  |  |  |  |  | Application |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Type | Hardness [GPa] | COF [-] dry vs. steel | Max. service temperature [C] | Thickness [µm] | Color | Steel < 1000 MPa | Steel > 1000 MPa | Steel 33- 55 HRC | Steel > 60 HRC | Stainless steel | Cast iron | Al alloys | Non-ferrous metals | Drilling | Milling | Turning | Shaping | Decorative | Forming | Threading | Tribology | Coinage |
| ARC coatings |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| TiN | 24-30 | 0.40 | 500 | 1-5 | gold |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| TiCN | 27-32 | 0.20 | 450 | 1-4 | copper to grey |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CrN | 21-25 | 0.60 | 650 | 1-6 | silver-grey |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CrCN | 22-26 | 0.60 | 650 | 1-6 | bright grey |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ZrN | 22-24 | 0.60 | 500 | 1-4 | white-gold |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| TiAlN | 32-34 | 0.50 | 700 | 1-4 | purple |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| AlTiN | 33-35 | 0.60 | 850 | 1-4 | dark grey-black |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KTRN I | 32-35 | 0.60 | 900 | 1-3 | anthracite |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KTRN II | 32-35 | 0.55 | 950 | 1-3 | aubergine-grey |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CRONAL | 30-32 | 0.65 | 1000 | 1-4 | bright grey |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| AlCrN | 33-35 | 0.60 | 1000 | 1-4 | bright grey |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| SICRAL | 35-37 | 0.55 | 1000 | 1-4 | gold-brown |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| TiSiN | 35-38 | 0.55 | 1100 | 1-3 | gold-brown |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| LEGEND |  |  |  |  |  | Primary solution | Secondary solution |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |